Quotation Sheet

Date: 2019-12-08

To:

| Country |  |
| --- | --- |
| Company Name |  |
| Attn |  |
| Tel |  |
| Fax |  |
| Mob |  |
| Email |  |
| Quotation | FOB RUB 4 500 000.00 St. Peterburg port, Russia |
| Exchange rate | 1$=64 RUB |
| Notes | 1.Delivery time: 90 working days; |
|  | 3.Warranty:One year; whole-life time technical support; |
|  | 4. Payment terms: 70% as deposit, 25% before shipment, 5% as the balance; |
|  | 5.Validity of this offer: 30 working days; |

GX-P Series Flat Glass Tempering Furnace

Model No. GX-P0609(4-12mm)

- Appendix 1

Technical Specifications

1.1 Description of the equipment(unit: mm)

| Model No. | GX-P0609 |
| --- | --- |
| Equipment size (L*W*H) | 2800(width)*5800(length)mm |
| Floor space (L*W) | 2800(width)*5800(length)mm |
| Glass thickness | 4-12mm |
| Max loading area | 600*900mm |
| Min glass size | 100*100mm |
| Heating methods | Radiation |
| Suitable glass types | Off-line coated glass, on-line coated glass; Pattern glass, color glass; Clear float glass |
| Requested glass quality | No visible bubbles, impurities; Meet the national standards of high quality float glass; Glass shall be beveling, edging, washing and dry; |
| Finished product rate | Not less than 98% |
| Tempered glass quality standard | Better than national standard |
| Power consumption | Less than 4 kw/h/m2—6mm |
| Productivity | 12-14 Loads/H——6mm 9-11 Loads/H——8mm |

1.2  Glass specifications and acceptance standard of tempered glass

| Glass thickness & types | Bow | Edge waveness |
| --- | --- | --- |
| 6mm, clear glass | ≤2‰ | ≤0.13/300mm |
| 8mm, clear glass | ≤1.5‰ | ≤0.1/300mm |
| 10mm, clear glass | ≤1.5‰ | ≤0.1/300mm |
| 12mm, clear glass | ≤1.5‰ | ≤0.1/300mm |
| 15mm, clear glass | ≤1.5‰ | ≤0.1/300mm |
| Finished product rate （refined edging） | ≥98% |
| Full tempered granularity(50mm x 50mm) ≥ national standard |
| Standards: GB15763.2-2005, GB17841-2008, EN12150 etc. |

1.3 Technical specifications of corollary equipment(supplied by the buyer)

| Air pressure of the compressor: | ＞0.6MPa（supplied by the buyer） |
| --- | --- |
| Compressed air volume: | ＞1000L/min（supplied by the buyer） |
| Cables from transformer to the control cabinet and blowers | Supplied by the buyer |
| Power supply requests | Drawings will be provided by the seller, the grounding wires will be done by the buyer |

1.4 Installed power

| Items | Parameters | Notes |
| --- | --- | --- |
| Heating power | 32kW |  |
| Blower power | 30kW | with Siemens or Schneider inverter, save 30% blower power consumption |
| Rest | 15kW |  |
| Total power | 77kW | Actual power is 75% of the total power |
| Transformer | 63KVA | Provided by the buyer |

- Appendix 2

Equipment Structure & Manufacturing Standard

| Loading & Unloading Section |  | With light tubes to check the glass quality; Security socket for glass repair tools, more convenient; Store content box to put tools and other small stuffs for production; Driving motor with inverters, to transmit glass enter the furnace in high speed; With lifting table for large size glass loading; |
| --- | --- | --- |
| Heating section |  | Top heating section could go up and down by the lifting system which installed on top of the furnace, lifting height could be 500mm, which is convenient for cleaning the furnace; Insulation is high density ceramic fiber board, the surface will be coated by high temperature resistant glue, in the last, all insulation will be covered by magnetized high aluminum plates, which could prevent any fallings to the glass; High quality insulation material, from 25℃ to 700℃，takes about 3-4 hours, temperature falling down per hour about 15℃; |
|  |  | Double belts driving system, better synchronism and safer; |
|  |  | Heating elements material is from Beijing Shougang Co.,Ltd; Arrangements of heating elements will be different according to different sizes; Easily installation and convenient for maintenance and replacement; Heating elements are independent, maintenance or replacement won’t effect other heating elements; Temperature detection is done by separated thermocouple and each temperature and heating power could be set independent and separately, which could ensure the temperature side furnace is more even; |
|  |  | In the bottom of the heating section, above the heating elements, there are radiation plates, which is corrugated shape, no deformation under high temperature Broken glass pieces will fall down on the radiation plates, easily and convenient for cleaning; |
|  |  | 1.Ceramic bricks, customized, precisely diameter, small gap, durable, better insulation performance, easily replacement; |
|  |  | Famous brand and top quality ceramic rollers; Double belts driving system; Inverters control the speed of motor, better synchronism and stable; Provide the installation frames for ceramic rollers, easy and convenient for remove and install the ceramic rollers; Sealed bearings; |
|  |  | Driving shaft is chrome plated, high surface quality, good straightness; V-groove in the 45° length direction of the shaft, to fix the belts pulley, easily for installation of the pulley; Shaft end is outer square and couplings are inner square, connection is more strong, no shake between shafts driving, which could avoid the glass crashed together; |
| Flat quenching section(Automatic type) |  | Top & bottom quenching section could be adjusted the height separately, which is more convenient for adjust the flatness accordingly; The air box is bent by cold plate, one time formed; Rollers are high quality and thicker steel rod, high temperature resistance Kevlar rope stick on the rollers by high temperature glue, which are also baked by heat treatment; Chain driving system, better synchronism. |
|  |  | Small air box can be cleaned fast and convenient, removable and separately dam-boards on each small air box |
|  |  | Blower is unit frame, easy and convenient for installation; Cushion pad support; |
| Control system |  | Wiring configurations: All wires and electrical components and cables are with CE standard; Power cables(including the cables between inverter and blower) shall be provided by the buyer; |
|  |  | PLC: Omron, Japan Stable and reliable program, friendly human-computer interface; Abnormal alarm functions(like encoder problems, parameters setting problems etc) and records of alarms, which could be as a reference for maintenance for after-sales technicians; |
|  |  | Temperature control system: Temperature control is done by modules, which is better for interference rejection; More accuracy and stable for temperature control; According to different glass size, the temperature curve will be set and each heating element temperature and heating power could be set separately; Module is like a small computer, signal of temperature will be collected and access to the control module, then the heating elements on/off will be controlled accordingly(like the temperature setting and heating power setting), control accuracy is within 3 ℃； Temperature detection is done by I-7018(temperature detection module), strong interference rejection, high accuracy temperature detection; Heating elements on/off adopt SSR, stable and reliable, no noise; |
|  |  | Operation cabinet: Separately operation cabinet for industrial computer, which is better for interference rejection; Industrial computer being used; By different operations or failures, pop-up windows come up and show the errors to remind the operator; To avoid wrong operations, there is strict authorization limit for these parameters which may effect the normal production; different authorization limit for different operators(technicians or operators); Complete monitoring function for almost all the sensors and components; Automatic parameters saving and upgrade; Automatic monitoring on thermocouples, once any of them breaks down, there will be error warning showing up and reminding which one is broken down; |
| After-sales service |  | Scanning code for each machine. Any problems with the machine, scan this code and write the services requests or comments for services technicians, Gangxin head-office will receive all information from customer’s end, which is better to control the services quality and efficient. |

- Appendix 3

Main Configurations for Mechanical & Electrical Components

3.1 Mechanical Components

| No. | Items | Brands/Origional |
| --- | --- | --- |
| 1 | Ceramic rollers | Chuangxin, China |
| 2 | Driving belts(ceramic rollers driving system) | Barbieri, Italy |
| 3 | Insulation material(high aluminum insulation board) | Sinosteel Luoyang Institute of Refractories Research Co.,Ltd |
| 4 | Kevlar Rope | Dupont, USA(Material brand) |
| 5 | Quenching blower | Wendeng,Shandong/Fochan, Foshan |
| 6 | Cycloid pin speed reducer | Guomao, Changzhou |
| 7 | Worm gear reducer | Zhujiang, Foshan |
| 8 | Pneumatic component | SAZN,Zhejiang |
| 9 | Bearing | Haerbin/Wafangdian/Luoyang |
| 10 | Section bar | Wuhan Iron and Steel Group |
| 11 | Heating elements | Shougang Group(Beijing) |
| 12 | Rubber rollers | Xinhe, Hebei |
| 13 | Chains | Huagang, Zhejiang |
| 14 | Ceramic pipes | Xingyang, Henan |
| 15 | Aluminum profile | Zhengzhou, Henan |
| 16 | Driving chain wheel | Customized |
| 17 | Steel rollers(quench driving) | Xinhe, Hebei |
| 18 | Fireproof air duct | Hengshui, Hebei |
| 19 | Universal wheel | Hengshui, Hebei |

3.2 Electrical Components

| No. | Items | Models | Brands/Original |
| --- | --- | --- | --- |
| 1 | PLC | CP1H-40DR-A | Omron, Japan |
| 2 | 40 points extended module | CPM1A-40EDR | Omron, Japan |
| 3 | 20 points extended module | CPM1A-20EDR1 | Omron, Japan |
| 4 | Analog output module | CPM1A-DA041 | Omron, Japan |
| 5 | Encoder | E6B2 | Omron, Japan |
| 6 | optoelectronic switch | E3Z-T61 | Omron, Japan |
| 7 | Proximity switch | 3P18 | Omron, Japan |
| 8 | Industrial computer |  | Siemens, Germany |
| 9 | Temperature detection module | I-7018R | ICP-DAS, Taiwan |
| 10 | Temperature detection module baseplate | I-7520R | ICP-DAS, Taiwan |
| 11 | Digital output module | I-8057-G | ICP-DAS, Taiwan |
| 12 | Digital module CPU | I-8411 | ICP-DAS, Taiwan |
| 13 | Monitor | 19 inch, LED | Philips, Holland |
| 14 | Inverters for driving motors | ATV series | Schneider, Germany |
| 15 | Thermocouples | WRGKK-131 | Chuangyi, Chongqing |
| 16 | Solid State Relay | Ximandun | Ximandun, Beijing;Gute,Wuxi |
| 17 | Isolation transformer | 220V→ 24V | Omron, Japan |
| 18 | Moulded case breaker | NM1-60S | CHNT, China |
| 19 | Middle relay | RXM4LB | Schneider, Germany |
| 20 | Miniature breaker | C65N | Schneider, Germany |
| 21 | A.C. contactor | 3TB4022 | Siemens, Germany |
| 22 | Thermal protection breaker | GV2-ME | Schneider, Germany |
| 23 | Rotary knob | ZB2 | Schneider, Germany |
| 24 | Button | ZB2 | Schneider, Germany |
| 25 | Indicator light | XB2 | Schneider, Germany |
| 26 | A.C. Voltmeter | 42L6-V | Xuji Group, China |
| 27 | A.C. Ammeter | 42C3-V | Xuji Group, China |
| 28 | Temperature controlled meter | Yudian | Yudian, Xiamen |
| 29 | Air-pressure meter | Yudian | Yudian, Xiamen |
| 30 | Inverters for quenching blower |  | Siemens/Schneider, Germany |
| 31 | UPS | Power-supply back up | Kehua/Invt,China |

- Appendix 4

SPARE PARTS LISTS

| No. | CN Items | EN Items | Model | Unit | Quantity |
| --- | --- | --- | --- | --- | --- |
| Loading/unloading section |
| 1 | 辊道轴承 | Roller bearing | Design size | Set | 2 |
| 2 | 双排链条 | double-line chain | 06B-2 | meter | 1.5 |
| 3 | 芳纶绳 | Kevlar rope | 3×10 | meter | 50 |
| 4 | 万向轮（带座） | versatile wheel with seat | Design size | Set | 10 |
| 5 | 带座轴承 | Bearing with seat | Design size | Set | 2 |
| 6 | 辊道链轮 | chain wheel | Design size | piece | 2 |
| Heating section |
| 7 | 热电偶 | thermocouple | Design size | piece | 3 |
| 8 | O型皮带 | O belts | Design size | piece | 10 |
| 9 | 陶瓷辊道主动端轴承 | Bearing for main drive end | Design size | Set | 2 |
| 10 | 陶瓷辊道被动端轴承 | Bearing for passive end | Design size | Set | 2 |
| 11 | 炉丝穿线瓷管 | porcelain pipe for heaters | Design size | piece | 5 |
| 12 | 上部热电偶T瓷管 | Ceramic Tube for top thermocouples (T type) | Design size | Piece | 5 |
| 13 | 下部热电偶T瓷管 | Ceramic pipe for bottom thermocouples(T type) | Design size |  | 5 |
| 14 | 上部瓷砖 | Top Ceramic block | Design size | Piece | 2 |
| 15 | 下部瓷砖 | Bottom Ceramic block | Design size | Piece | 2 |
| 16 | 上部炉丝T型管 | T ceramic tube for top heaters | Design size | Piece | 5 |
| 17 | 下部炉丝T瓷管 | T ceramic tube for bottom heaters | Design size |  | 5 |
| 18 | 上部炉丝 | Top heaters | Design size | Piece | 2 |
| 19 | 下部炉丝 | Bottom heaters | Design size | Piece | 2 |
| 20 | 陶瓷辊道 | Ceramic rollers | Design size | piece | 1 |
| 21 | Φ8 PU管 | Φ8 PU tube | Φ8 | meter | 10 |
| 22 | Φ6 PU管 | Φ6 PU tube | Φ6 | meter | 10 |
| 23 | 铜螺栓 | Copper bolt | Design size | set | 10 |
| 24 | 固化胶 | Case hardening glue | Design size | kg | 2 |
| 25 | 传动轴轴承 | Bearing for driving shaft | Design size | Set | 1 |
| Flat quench section |
| 26 | 链条 | Chain | 06B-2 | meter | 1.5 |
| 27 | 链条活接 | Chain joint | 06B-2/06B-3 | pcs | 2 |
| 28 | 链条 | Chain | 10A-1 | meter | 1.5 |
| 29 | 帆布管 | Canvas duct | Design size | piece | 1 |
| 30 | 传动主动端辊道轴承 | Bearing for main drive end | Design size | Set | 1 |
| 31 | 传动被动端辊道轴承 | Bearing for passive end | Design size | Set | 1 |
| Electrical system |
| 32 | 按钮 | button | ZB2-BA4C+ZB2-BZ101C | pieces | 2 |
| 33 | 旋钮 | Rotary knob | ZB2-BD2C+ZB2-BZ101C |  | 2 |
| 34 | 指示灯 | indicator light | AC220V XB2-BVM3LC | pieces | 2 |
| 35 | 交流接触器 | AC contactor | 3TB4022 AC220V | pieces | 1 |
| 36 | 中间继电器 | midst relay | RXM4LB2BD 24V | piece | 4 |
| 37 | 断路器 | Breaker | IC65N 3P 10A | Piece | 1 |
| 38 | 断路器 | Breaker | IC65N 2P 10A | Piece | 1 |
| 39 | 断路器 | Breaker | GV2-ME 3P 6A | Piece | 1 |
| 40 | 指示灯 | Indicator light | AC220V XB2-BVM3LC | piece | 2 |
| 41 | 保险 | Fuse | 4A | piece | 3 |
| 42 | 保险 | Fuse | 2A | Piece | 3 |
| 43 | 快熔 | fast fuse | Design size | piece | 4 |
| 44 | 固态继电器 | Solid state relay | Design size | piece | 5 |
| 45 | 散热风扇 | Fan | Control cabinet | piece | 1 |
| 46 | 接近开关 | Proximity switch | E2E-X10ME | piece | 1 |
| 47 | 光电开关 | Photoelectric switches | E3Z-T61 | couple | 1 |
| 48 | 限位开关 | Limit switch | Design size | piece | 1 |
| 49 | 风机联轴器垫 | Damping padding for coupling in blower | Design size | set | 1 |